## Slide 1: DOE-Parameters for DEM model
Outputs:
Surface Roughness (mm)
Variance Surface roughness (mm)
Solid Fraction
Variance Solid Fraction
Coordinate Number
Variance Coordinate Number

## Slide 2: Analysis Region

## Slide 3: Solid Fraction (unitless)
Convex Hull over the particle centers
  Assume this pattern repeats otherwise solid fraction is much lower
  Outside compute: 0.543
  Center compute: 0.578

## Slide 4: Roughness (mm)
Height map in mm
For each transverse direction to spreading (evey pixel column) compute standard deviation in height
Average these to get roughness value
STD(height)
STD(height)
STD(height)
STD(height)
STD(height)
STD(height)
Average(STD)

## Slide 5: Metric Comparison
Chart: Solid Fraction
| 0.57153998686070195 | 0.56520520608881297 | 0.57847557392621496 | 0.57460908697132496 | 0.57380013900016702 | 0.56245218690107202 | 0.56468058440112301 | 0.59099446788374099 | 0.58903283231749404 | 0.57773895425430399 | 0.57693223671015503 | 0.56303383195501999 | 0.56030555816926098 | 0.56213982930544903 | 0.54101296097562701 | 0.534245265414522 | 0.52095714087074996 | 0.60849808636635505 | 0.594793763559887 | 0.59617468741846202 | 0.58409892721387202 | 0.58059960130673305 | 0.57869161591311202 | 0.56324144507152296 | 0.56439479484212896 | 0.562951633363166 | 0.58384422301022298
mean_coordination_number | 2.7929 | 2.7038 | 3.3653 | 2.9381 | 2.7855 | 2.5655 | 2.8596 | 3.5354 | 3.7405 | 3.3726 | 3.3875 | 2.6594 | 2.7416 | 2.7688 | 2.3228 | 2.5208 | 2.4655 | 4.1339 | 3.9861 | 3.7309 | 3.439 | 3.2411 | 2.9734 | 3.1249 | 2.9251 | 2.7819 | 3.4318
Chart: Roughness
| 0.50711548328399603 | 0.52132195234298695 | 0.50830173492431596 | 0.51266807317733698 | 0.51586067676544101 | 0.52016490697860696 | 0.52341127395629805 | 0.48465475440025302 | 0.486221224069595 | 0.52112990617751997 | 0.52574896812438898 | 0.54942375421524003 | 0.56300961971282903 | 0.573819279670715 | 0.56135582923889105 | 0.57321560382842995 | 0.58188009262084905 | 0.41715237498283297 | 0.43209728598594599 | 0.43895730376243502 | 0.445480376482009 | 0.44782698154449402 | 0.45873239636421198 | 0.469378381967544 | 0.46229028701782199 | 0.46678137779235801 | 0.49495601654052701
mean_clipped_hull_relative_density | 0.57154 | 0.56521 | 0.57848 | 0.57461 | 0.5738 | 0.56245 | 0.56468 | 0.59099 | 0.58903 | 0.57774 | 0.57693 | 0.56303 | 0.56031 | 0.56214 | 0.54101 | 0.53425 | 0.52096 | 0.6085 | 0.59479 | 0.59617 | 0.5841 | 0.5806 | 0.57869 | 0.56324 | 0.56439 | 0.56295 | 0.58384

## Slide 6: Metric to Variance
Chart: Roughness (mm)
| 0.48642283678054798 | 0.50558012723922696 | 0.49400648474693298 | 0.49920472502708402 | 0.48960104584693898 | 0.51206338405609098 | 0.509221851825714 | 0.481332898139953 | 0.49170523881912198 | 0.50709044933319003 | 0.50785231590270996 | 0.50962579250335605 | 0.52944523096084595 | 0.52235591411590498 | 0.54279243946075395 | 0.55546408891677801 | 0.55156433582305897 | 0.419630616903305 | 0.43031713366508401 | 0.432635277509689 | 0.43110749125480602 | 0.432525604963302 | 0.440867960453033 | 0.44916778802871699 | 0.44825577735900801 | 0.45269972085952698 | 0.48705667257308899
transverse_rms_roughness_variance_mm2 | 0.0057188 | 0.0071827 | 0.0067032 | 0.0068395 | 0.0062662 | 0.0089903 | 0.0078345 | 0.0068059 | 0.0070451 | 0.0086089 | 0.0082768 | 0.0061799 | 0.0069902 | 0.0074228 | 0.0084907 | 0.0097432 | 0.0094134 | 0.0046334 | 0.0039389 | 0.0041445 | 0.004772 | 0.0043112 | 0.0044192 | 0.0054647 | 0.0049773 | 0.0062381 | 0.0071368
Chart: Solid Fraction
| 0.59260562179970599 | 0.58369885216436801 | 0.58607042270051102 | 0.58937059686003801 | 0.59457365927138295 | 0.57658878569431704 | 0.58085317398910696 | 0.59556769614805105 | 0.59138419659262897 | 0.58728365421999995 | 0.58331561888768502 | 0.58847359759968598 | 0.58288866584195398 | 0.58758785057812701 | 0.56592220444855901 | 0.55751440150333498 | 0.55646472641936295 | 0.61222335888003998 | 0.59677544582131503 | 0.60097933944340998 | 0.59744984156745995 | 0.59767670412076002 | 0.59566609802963399 | 0.58034476268385304 | 0.58101955404462802 | 0.58062882164240004 | 0.58989301700498198
variance_clipped_hull_relative_density | 0.0014899 | 0.0021502 | 0.00076879 | 0.0017192 | 0.0014486 | 0.0029678 | 0.0026641 | 0.00089776 | 0.00095771 | 0.00090245 | 0.0010068 | 0.0015184 | 0.0018238 | 0.0017822 | 0.0025386 | 0.0029534 | 0.0030484 | 0.00072938 | 0.00065523 | 0.00090362 | 0.001085 | 0.0011337 | 0.001144 | 0.0016989 | 0.0018705 | 0.0021115 | 0.0008619
Chart: Coordinate Number
| 4.3801341156747604 | 4.1498790271233901 | 4.52135157545605 | 4.3676172294475597 | 4.3395341313490698 | 4.0730172052035201 | 4.1544153441729099 | 4.5931401537551704 | 4.5330686019444002 | 4.43989005736137 | 4.4567099567099504 | 4.2684008276677501 | 4.2156317578004296 | 4.1439771917319996 | 3.9555901830931002 | 3.8496628322094399 | 3.7766911165444101 | 5.10086476815267 | 4.8688915375446902 | 4.7544001173364601 | 4.6669133974833397 | 4.6466187050359702 | 4.6359654178674301 | 4.4025727359060696 | 4.3805166333047296 | 4.4065872302158198 | 4.5653782134270298
coordination_number_variance | 5.0551 | 4.7297 | 4.3555 | 5.104 | 5.2563 | 4.924 | 4.8002 | 4.51 | 3.6982 | 3.7067 | 3.719 | 3.9173 | 3.893 | 4.2359 | 3.6069 | 3.9112 | 4.0871 | 5.8743 | 5.0785 | 5.7331 | 5.7718 | 5.7466 | 5.7151 | 5.3179 | 5.2764 | 5.471 | 4.3724

## Slide 7: Coordinate Number
Chart: Roller Diameter (mm)
| 100 | 50 | 150 | 50 | 150 | 100 | 150 | 50 | 50 | 100 | 150 | 50 | 100 | 150 | 50 | 100 | 150 | 50 | 100 | 150 | 50 | 100 | 150 | 50 | 100 | 150 | 100
 | 4.3801 | 4.1499 | 4.5214 | 4.3676 | 4.3395 | 4.073 | 4.1544 | 4.5931 | 4.5331 | 4.4399 | 4.4567 | 4.2684 | 4.2156 | 4.144 | 3.9556 | 3.8497 | 3.7767 | 5.1009 | 4.8689 | 4.7544 | 4.6669 | 4.6466 | 4.636 | 4.4026 | 4.3805 | 4.4066 | 4.5654
Chart: Roller Speed (mm/s)
| 300 | 500 | 100 | 300 | 300 | 500 | 500 | 100 | 100 | 100 | 100 | 300 | 300 | 300 | 500 | 500 | 500 | 100 | 100 | 100 | 300 | 300 | 300 | 500 | 500 | 500 | 100
 | 4.3801 | 4.1499 | 4.5214 | 4.3676 | 4.3395 | 4.073 | 4.1544 | 4.5931 | 4.5331 | 4.4399 | 4.4567 | 4.2684 | 4.2156 | 4.144 | 3.9556 | 3.8497 | 3.7767 | 5.1009 | 4.8689 | 4.7544 | 4.6669 | 4.6466 | 4.636 | 4.4026 | 4.3805 | 4.4066 | 4.5654
Chart: % small particle
| 50 | 50 | 50 | 50 | 50 | 50 | 50 | 50 | 25 | 25 | 25 | 25 | 25 | 25 | 25 | 25 | 25 | 75 | 75 | 75 | 75 | 75 | 75 | 75 | 75 | 75 | 50
 | 4.3801 | 4.1499 | 4.5214 | 4.3676 | 4.3395 | 4.073 | 4.1544 | 4.5931 | 4.5331 | 4.4399 | 4.4567 | 4.2684 | 4.2156 | 4.144 | 3.9556 | 3.8497 | 3.7767 | 5.1009 | 4.8689 | 4.7544 | 4.6669 | 4.6466 | 4.636 | 4.4026 | 4.3805 | 4.4066 | 4.5654

## Slide 8: Coordinate Number Variance
Chart: roller speed (mm/s)
| 300 | 500 | 100 | 300 | 300 | 500 | 500 | 100 | 100 | 100 | 100 | 300 | 300 | 300 | 500 | 500 | 500 | 100 | 100 | 100 | 300 | 300 | 300 | 500 | 500 | 500 | 100
coordination_number_variance | 5.0551 | 4.7297 | 4.3555 | 5.104 | 5.2563 | 4.924 | 4.8002 | 4.51 | 3.6982 | 3.7067 | 3.719 | 3.9173 | 3.893 | 4.2359 | 3.6069 | 3.9112 | 4.0871 | 5.8743 | 5.0785 | 5.7331 | 5.7718 | 5.7466 | 5.7151 | 5.3179 | 5.2764 | 5.471 | 4.3724
Chart: roller size (mm)
| 100 | 50 | 150 | 50 | 150 | 100 | 150 | 50 | 50 | 100 | 150 | 50 | 100 | 150 | 50 | 100 | 150 | 50 | 100 | 150 | 50 | 100 | 150 | 50 | 100 | 150 | 100
coordination_number_variance | 5.0551 | 4.7297 | 4.3555 | 5.104 | 5.2563 | 4.924 | 4.8002 | 4.51 | 3.6982 | 3.7067 | 3.719 | 3.9173 | 3.893 | 4.2359 | 3.6069 | 3.9112 | 4.0871 | 5.8743 | 5.0785 | 5.7331 | 5.7718 | 5.7466 | 5.7151 | 5.3179 | 5.2764 | 5.471 | 4.3724
Chart: % small powder
| 50 | 50 | 50 | 50 | 50 | 50 | 50 | 50 | 25 | 25 | 25 | 25 | 25 | 25 | 25 | 25 | 25 | 75 | 75 | 75 | 75 | 75 | 75 | 75 | 75 | 75 | 50
coordination_number_variance | 5.0551 | 4.7297 | 4.3555 | 5.104 | 5.2563 | 4.924 | 4.8002 | 4.51 | 3.6982 | 3.7067 | 3.719 | 3.9173 | 3.893 | 4.2359 | 3.6069 | 3.9112 | 4.0871 | 5.8743 | 5.0785 | 5.7331 | 5.7718 | 5.7466 | 5.7151 | 5.3179 | 5.2764 | 5.471 | 4.3724

## Slide 9: Relative Density (solid fraction)
Chart: % small powder
| 50 | 50 | 50 | 50 | 50 | 50 | 50 | 50 | 25 | 25 | 25 | 25 | 25 | 25 | 25 | 25 | 25 | 75 | 75 | 75 | 75 | 75 | 75 | 75 | 75 | 75 | 50
 | 0.59261 | 0.5837 | 0.58607 | 0.58937 | 0.59457 | 0.57659 | 0.58085 | 0.59557 | 0.59138 | 0.58728 | 0.58332 | 0.58847 | 0.58289 | 0.58759 | 0.56592 | 0.55751 | 0.55646 | 0.61222 | 0.59678 | 0.60098 | 0.59745 | 0.59768 | 0.59567 | 0.58034 | 0.58102 | 0.58063 | 0.58989
Chart: Roller Speed (mm/s)
| 300 | 500 | 100 | 300 | 300 | 500 | 500 | 100 | 100 | 100 | 100 | 300 | 300 | 300 | 500 | 500 | 500 | 100 | 100 | 100 | 300 | 300 | 300 | 500 | 500 | 500 | 100
 | 0.59261 | 0.5837 | 0.58607 | 0.58937 | 0.59457 | 0.57659 | 0.58085 | 0.59557 | 0.59138 | 0.58728 | 0.58332 | 0.58847 | 0.58289 | 0.58759 | 0.56592 | 0.55751 | 0.55646 | 0.61222 | 0.59678 | 0.60098 | 0.59745 | 0.59768 | 0.59567 | 0.58034 | 0.58102 | 0.58063 | 0.58989
Chart: Roller Diameter (mm)
| 100 | 50 | 150 | 50 | 150 | 100 | 150 | 50 | 50 | 100 | 150 | 50 | 100 | 150 | 50 | 100 | 150 | 50 | 100 | 150 | 50 | 100 | 150 | 50 | 100 | 150 | 100
 | 0.59261 | 0.5837 | 0.58607 | 0.58937 | 0.59457 | 0.57659 | 0.58085 | 0.59557 | 0.59138 | 0.58728 | 0.58332 | 0.58847 | 0.58289 | 0.58759 | 0.56592 | 0.55751 | 0.55646 | 0.61222 | 0.59678 | 0.60098 | 0.59745 | 0.59768 | 0.59567 | 0.58034 | 0.58102 | 0.58063 | 0.58989

## Slide 10: Relative Density Variance
Chart: % small powder
| 50 | 50 | 50 | 50 | 50 | 50 | 50 | 50 | 25 | 25 | 25 | 25 | 25 | 25 | 25 | 25 | 25 | 75 | 75 | 75 | 75 | 75 | 75 | 75 | 75 | 75 | 50
variance_clipped_hull_relative_density | 0.0014899 | 0.0021502 | 0.00076879 | 0.0017192 | 0.0014486 | 0.0029678 | 0.0026641 | 0.00089776 | 0.00095771 | 0.00090245 | 0.0010068 | 0.0015184 | 0.0018238 | 0.0017822 | 0.0025386 | 0.0029534 | 0.0030484 | 0.00072938 | 0.00065523 | 0.00090362 | 0.001085 | 0.0011337 | 0.001144 | 0.0016989 | 0.0018705 | 0.0021115 | 0.0008619
Chart: roller speed (mm/s)
| 300 | 500 | 100 | 300 | 300 | 500 | 500 | 100 | 100 | 100 | 100 | 300 | 300 | 300 | 500 | 500 | 500 | 100 | 100 | 100 | 300 | 300 | 300 | 500 | 500 | 500 | 100
variance_clipped_hull_relative_density | 0.0014899 | 0.0021502 | 0.00076879 | 0.0017192 | 0.0014486 | 0.0029678 | 0.0026641 | 0.00089776 | 0.00095771 | 0.00090245 | 0.0010068 | 0.0015184 | 0.0018238 | 0.0017822 | 0.0025386 | 0.0029534 | 0.0030484 | 0.00072938 | 0.00065523 | 0.00090362 | 0.001085 | 0.0011337 | 0.001144 | 0.0016989 | 0.0018705 | 0.0021115 | 0.0008619
Chart: roller size (mm)
| 100 | 50 | 150 | 50 | 150 | 100 | 150 | 50 | 50 | 100 | 150 | 50 | 100 | 150 | 50 | 100 | 150 | 50 | 100 | 150 | 50 | 100 | 150 | 50 | 100 | 150 | 100
variance_clipped_hull_relative_density | 0.0014899 | 0.0021502 | 0.00076879 | 0.0017192 | 0.0014486 | 0.0029678 | 0.0026641 | 0.00089776 | 0.00095771 | 0.00090245 | 0.0010068 | 0.0015184 | 0.0018238 | 0.0017822 | 0.0025386 | 0.0029534 | 0.0030484 | 0.00072938 | 0.00065523 | 0.00090362 | 0.001085 | 0.0011337 | 0.001144 | 0.0016989 | 0.0018705 | 0.0021115 | 0.0008619

## Slide 11: Surface Roughness
Chart: % small particle
| 50 | 50 | 50 | 50 | 50 | 50 | 50 | 50 | 25 | 25 | 25 | 25 | 25 | 25 | 25 | 25 | 25 | 75 | 75 | 75 | 75 | 75 | 75 | 75 | 75 | 75 | 50
 | 0.48642 | 0.50558 | 0.49401 | 0.4992 | 0.4896 | 0.51206 | 0.50922 | 0.48133 | 0.49171 | 0.50709 | 0.50785 | 0.50963 | 0.52945 | 0.52236 | 0.54279 | 0.55546 | 0.55156 | 0.41963 | 0.43032 | 0.43264 | 0.43111 | 0.43253 | 0.44087 | 0.44917 | 0.44826 | 0.4527 | 0.48706
Chart: Roller Speed (mm/s)
| 300 | 500 | 100 | 300 | 300 | 500 | 500 | 100 | 100 | 100 | 100 | 300 | 300 | 300 | 500 | 500 | 500 | 100 | 100 | 100 | 300 | 300 | 300 | 500 | 500 | 500 | 100
 | 0.48642 | 0.50558 | 0.49401 | 0.4992 | 0.4896 | 0.51206 | 0.50922 | 0.48133 | 0.49171 | 0.50709 | 0.50785 | 0.50963 | 0.52945 | 0.52236 | 0.54279 | 0.55546 | 0.55156 | 0.41963 | 0.43032 | 0.43264 | 0.43111 | 0.43253 | 0.44087 | 0.44917 | 0.44826 | 0.4527 | 0.48706
Chart: Roller Diameter (mm)
| 100 | 50 | 150 | 50 | 150 | 100 | 150 | 50 | 50 | 100 | 150 | 50 | 100 | 150 | 50 | 100 | 150 | 50 | 100 | 150 | 50 | 100 | 150 | 50 | 100 | 150 | 100
 | 0.48642 | 0.50558 | 0.49401 | 0.4992 | 0.4896 | 0.51206 | 0.50922 | 0.48133 | 0.49171 | 0.50709 | 0.50785 | 0.50963 | 0.52945 | 0.52236 | 0.54279 | 0.55546 | 0.55156 | 0.41963 | 0.43032 | 0.43264 | 0.43111 | 0.43253 | 0.44087 | 0.44917 | 0.44826 | 0.4527 | 0.48706

## Slide 12: Roughness Variance
Chart: % small powder
| 50 | 50 | 50 | 50 | 50 | 50 | 50 | 50 | 25 | 25 | 25 | 25 | 25 | 25 | 25 | 25 | 25 | 75 | 75 | 75 | 75 | 75 | 75 | 75 | 75 | 75 | 50
transverse_rms_roughness_variance_mm2 | 0.0057188 | 0.0071827 | 0.0067032 | 0.0068395 | 0.0062662 | 0.0089903 | 0.0078345 | 0.0068059 | 0.0070451 | 0.0086089 | 0.0082768 | 0.0061799 | 0.0069902 | 0.0074228 | 0.0084907 | 0.0097432 | 0.0094134 | 0.0046334 | 0.0039389 | 0.0041445 | 0.004772 | 0.0043112 | 0.0044192 | 0.0054647 | 0.0049773 | 0.0062381 | 0.0071368
Chart: Roller Speed (mm/s)
| 300 | 500 | 100 | 300 | 300 | 500 | 500 | 100 | 100 | 100 | 100 | 300 | 300 | 300 | 500 | 500 | 500 | 100 | 100 | 100 | 300 | 300 | 300 | 500 | 500 | 500 | 100
transverse_rms_roughness_variance_mm2 | 0.0057188 | 0.0071827 | 0.0067032 | 0.0068395 | 0.0062662 | 0.0089903 | 0.0078345 | 0.0068059 | 0.0070451 | 0.0086089 | 0.0082768 | 0.0061799 | 0.0069902 | 0.0074228 | 0.0084907 | 0.0097432 | 0.0094134 | 0.0046334 | 0.0039389 | 0.0041445 | 0.004772 | 0.0043112 | 0.0044192 | 0.0054647 | 0.0049773 | 0.0062381 | 0.0071368
Chart: Roller Size (mm)
| 100 | 50 | 150 | 50 | 150 | 100 | 150 | 50 | 50 | 100 | 150 | 50 | 100 | 150 | 50 | 100 | 150 | 50 | 100 | 150 | 50 | 100 | 150 | 50 | 100 | 150 | 100
transverse_rms_roughness_variance_mm2 | 0.0057188 | 0.0071827 | 0.0067032 | 0.0068395 | 0.0062662 | 0.0089903 | 0.0078345 | 0.0068059 | 0.0070451 | 0.0086089 | 0.0082768 | 0.0061799 | 0.0069902 | 0.0074228 | 0.0084907 | 0.0097432 | 0.0094134 | 0.0046334 | 0.0039389 | 0.0041445 | 0.004772 | 0.0043112 | 0.0044192 | 0.0054647 | 0.0049773 | 0.0062381 | 0.0071368

## Slide 13: Model Comparison
Using cross-validation
  10% validation holdout
  10% test holdout
  80% training
FCNN overfits on validation
Random forest performs best overall

## Slide 14: Model Prediction
Held out performance
Normalized RMSE should be compared to 1 for random predictor
Output | Normalized RMSE | R² | Physical RMSE | Physical MAE
Mean roughness | 0.1924 | 0.9553 | 0.0076 | 0.0061
Roughness variance | 0.4228 | 0.8004 | 0.0007 | 0.0005
Mean relative density | 0.4250 | 0.7013 | 0.0051 | 0.0042
Relative-density variance | 0.3240 | 0.8635 | 0.0002 | 0.0002
Mean coordination number | 0.2972 | 0.8970 | 0.0846 | 0.0584
Coordination-number variance | 0.3927 | 0.8523 | 0.2899 | 0.2203